Poly(3-hydroxybutyrate-co-3-hydroxyvalerate) produced by Azotobacter vinelandii: Synthesis and characterization.

Viviana Urtuviaa, Andrés Péreza, Alvaro Díaz-Barreraa.

a Pontificia Universidad Católica de Valparaíso, Escuela de Ingenieria Bioquímica, Avenida Brasil 2147 Casilla 4059, Valparaíso, Chile.

Email: viviana.urtuvia@pucv.cl

Unlike traditional plastics derived from fossil fuels, biopolymers offer a more sustainable alternative, as they have similar thermomechanical characteristics. The growing potential of sustainable materials such as polyhydroxyalkanoates presents an opportunity to promote the circular economy [1,2]. Among them, poly(3-hydroxybutyrate-co-3-hydroxyvalerate) (PHBV) has attracted substantial attention as a promising material for different industrial applications [2]. The bacterium Azotobacter vinelandii  produce PHBV by the addition of valerate during cellular growth [3]. In cultures in a bioreactor, the molar composition of PHBV is affected by agitation rate and modality of culture. In this study, PHBV production by A. vinelandii OP was evaluated  in extended batch cultures to agitation rates of 300 and 600 rpm. 3-hydroxyvalerate (3HV) fraction into the PHBV was measured using GC-MS and PHBV yield from sucrose (YPHBV/S) was determined. Staining with Nile Red was performed to observe through fluorescence microscopy the production of PHBV. The results indicate that under the conditions evaluated, a similar PHBV content (up to 61 ± 2 % w w-1) was obtained, however, different 3HV fractions were obtained. In cultures performed to 300 rpm a YPHBV/S of 0.17 g g-1 and 3HV fraction of 11.5 ± 1.4 mol % (at 96 h), whereas to 600 rpm a highest YPHBV/S (0.24 g g-1) and 3HV fraction of 7.6 ± 1.1 mol % was achieved (at 48 h). PHBV films containing 11.5 and 14.9 mol % 3HV (cell harvested at 96 h) from cultures performed at 300 and 600 rpm, were prepared through the conventional solvent-cast technique, and characterized through thermomechanical analysis. The TG graph analysis showed that the two PHBV films did not begin thermal decomposition until 293 °C, and there were no significant decreases in the Tonset and Tpeak (in °C) with increasing 3HV content, showing equal thermal stability. Overall, the results of this study will improve the understanding of the PHBV production by A. vinelandii OP and could be suitable for the production of biopolymer blends for different biotechnological applications.

Acknowledgements:

This research was supported and funded by the Agencia Nacional de Investigacion y Desarrollo, Chile (ANID) through FONDECYT Initiation 11230164 (VU) and FONDECYT Regular 1231075 (AD).The authors would like to thank to the HUB Ambiental UPLA for providing the GC-MS equipment.

Reference:

[1] V.V. Devadas, K.S. Khoo, W.Y. Chia, K.W. Chew, H.S.H. Munawaroh, M.K. Lam, J.W. Lim, Y.C. Ho, K.T. Lee, P.L. Show, Algae biopolumer towards sustainable circular economy, Bioresour. Technol. 325 (2021) 124702.

[2] M.L. Tebaldi, A.L.C. Maia, F. Poletto, F.V. de Andrade, D.C.F. Soares, Poly(-3-hydroxybutyrate-co-3-hydroxyvalerate) (PHBV): current advances in syhthesis methodologies, antitumor applications and biocompatibility, J.Drug Deliv. Sci. Technol. 51 (2019) 115-126.

[3] V. Urtuvia, N. Maturana, C. Peña, A. Díaz-Barrera, Accumulation of poly(3-hydroxybutyrate-co-3-hydroxyvalerate) by Azotobacter vinelandii with different 3HV fraction in shake flasks and bioreactor, Bioprocess Biosyst. Eng., 43(8) (2020) 1469-1478.